## Slide 1: Introduction to AMITEX_FFTP http://www.maisondelasimulation.fr/projects/amitex/html/index.html Application to the behavior of concretes submitted to thermo-hydro-mechanical loadings
L.Gélébart, F.Bernachy
CEA Saclay - DEN
Journée « utilisateurs MFRONT » / 20 Mai 2016 / EDF Saclay

## Slide 2: OUTLINE
ECCOMAS Congress 2016
5 - 10 JUNE 2016 Crete Island, Greece
European Congress on Computational Methods in Applied Sciences and Engineering
Minisymposium FFT : 17 presentations
Introduction FFT
AMITEX_FFTP code – main features and specificities
Application to concretes

## Slide 3: Introduction
  « FFT-based » methods (or « Lippman-Schwinger-based » methods)
3D Image
(regular grid)
+ Local behavior
+ Average loading
Stress, strain fields…
FFT-based method
Periodic BC
AMITEX_FFTP
AMITEX_FFTP
ADVANTAGES (vs standard FE code)
No mesh, Efficiency, Well-suited for parallelism

## Slide 4: Introduction
Problem to solve
Auxiliary problem
Application of the Green operator:
Simple product in Fourier space
Mura 1997
Solution for the Auxiliary Problem
Re-written problem
  « FFT-based » methods (or « Lippman-Schwinger-based » methods)
Moulinec-Suquet,1994

## Slide 5: INTRODUCTION
  Drawbacks of the « Basic Scheme » (MS1994)
Sensitivity to
élastic contrast
Sensitivity to
Reference Medium
Spurious oscillations
Uniaxial Strain

## Slide 6: New features IN AMITEX_FFTP
Reference Material Sensitivity
  Convergence Acceleration technique (~Krylov-based method)
Post-doc Franck Ouaki, 2014-2015
Elastic contrast Sentitivity
Used in FE-code CAST3M (Newton-Raphson)
Do not require the tangent behavior
Simple implementation

## Slide 7: New features IN AMITEX_FFTP
  Finite Strain extension
Post-doc Franck Ouaki, 2014-2015
+ Convergence
Acceleration
Technique
(see also Lahellec, Eisenlhor…)
Basic Scheme

## Slide 8: New features IN AMITEX_FFTP
  Modified Discrete Green operator
Post-doc Franck Ouaki, 2014-2015
Sensitivity to
elastic contrast
Classical Green Operator
Modified Green operator
Classical Green Operator
=> Continuous derivation
Modified Green Operator
=> Discrete derivation (average/voxel)
(see also Willot, Brisard, Kabel…)

## Slide 9: New features IN AMITEX_FFTP
  Modified Discrete Green operator
Classical Green Operator
Modified Green operator
Recent application in progress (PhD P.O Barrioz at CEA/DEN/DMN/SEMI) :
Uniaxial tensile test (10%), at RT (298K)
Finite strain, 1000 steps
Dislocation-based CP for FCC austenitic steels (316 stainless steel)
Spheric Porosity within a Single Crystal

## Slide 10: New features IN AMITEX_FFTP
  Distributed parallel MPI implementation
Polycrystal (voronoï), dislocation-based Crystal Plasticity, small perturbations
Cluster poincare (Maison de la Simulation)
Weak scalability
Number of nodes = N, Problem size = NxK0
Elasped time on 1 node : tref
Elapsed time on N nodes : tN
64 nodes
1024 cores
IDEALLY : tN = tref
1 node
16 cores
Strong scalability
Number of nodes = N, Problem size = K0
Elasped time on 1 node : tref
Elapsed time on N nodes : tN
64 nodes
1024 cores
IDEALLY : tref / tN = N
1 node
16 cores
Notes: Pourquoi prédire? Comment prédire?
Réponse macroscopique => modèle pour reproduire (pas simple) => un modèle pour prédire
Toute une école qui s’est développée autour de l’idée que pour pouvoir « mieux » prédire il fallait comprendre comment il se déformait
Microstructure et mécanismes : fondement de l’approche multi-échelles
Remonter ces informations vers la modélisation
La simulation numérique peut être une étape intermédiaire
Matériaux polycristallins, alliges de Zr ou les aciers, SiC/SiC, bétons

## Slide 11: APPLICATION TO CRYSTAL PLASTICITY
  EXEMPLE OF A MASSIVELY PARALLEL SIMULATION
42875 grains
10243 resolution
1024 cores
Strain distribution
Uniaxial tensile test (1%)
Small Perturbations, 100 steps
Dislocation-based CP (54 internal variables)

## Slide 12: EXEMPLES D’APPLICATION
FISSURE DANS UN POLYCRISTAL

## Slide 13: EXEMPLES D’APPLICATION
MOUSSE (coll. CEA – Le Ripault)

## Slide 14: New features vs « Basic scheme »
  AMITEX_FFTP
  http://www.maisondelasimulation.fr/projects/amitex/html/index.html
Efficient MPI implementation
Modified Green Operator
Basic Scheme + Convergence Acceleration
Small perturbations and Finite Strain
Mfront (http://tfel.sourceforge.net/)
code generator compatibility
A quite ROBUST and EFFICIENT code (VERY efficient compared to FE!)
Usage : from STANDALONE PC to HPC
Research & Education licence : OK
Available online : OK
Inputs :
one .xml file for
algorithm parameters
material coefficients
loading and output
vtk file(s) for the 3D image
Outputs :
    Average response
    Per phase av. and std dev
Fields (vtk files)